# Clay / Lime Poultice –

# Data Sheet

## Product

Womersley’s wet poultice is ready to use manufactured from either a wet clay or lime putty mix that simply requires ‘knocking-up’ prior to application.

Mix Ratio Clay Poultice – 1:5 Wet Clay and a selection of well washed grit sands 5mm down.  For custom mix ratios and aggregates please contact us.  It is made using our top-quality and locally sourced natural wet clay which is well seasoned prior to use.

Mix Ratio Lime Poultice – 1:4 Lime Putty and a selection of well washed sands 2mm down.  For custom mix ratios and aggregates please contact us.  Manufactured using mature lime putty.

## Usage

Clay or Lime Poultice are traditional cleaning material for drawing out deep seated contaminants and staining from the surface of masonry and sculptures.

The most common use is for desalination of historic masonry suffering from soluble salt-related decay. Once the poultice has dried out it can be removed and the walls rechecked for salt content. This procedure can be repeated until the salt levels are significantly reduced.

Generally 20mm of Poultice will reduce salt content by up to 50% .  This procedure can be repeated until salt levels are significantly reduced.

Manufactured on site in Yorkshire from well-seasoned wet clay plaster or mature lime putty and selected aggregates.

Coverage

## Coverage approx. 1m2 from 20kg at 10mm thick

## Advantages

- Quality controlled production.

- Consistency of mix ratio.

- 100% natural.

- Minimal carbon footprint.

- Significant removal of salts

## Surface Preparation

Suitable for application over stone and brick backgrounds.

## How to Mix

Womersley’s poultice is ready to use.  Any excess water on top of the tub should be poured away and the plaster knocked up.

How to Apply

Apply in the conventional manner with a hawk and trowel up to 20mm thick.

Curing and Why

The water contained in the poultice soaks slowly into the wall and dissolves salts, soiling and contaminants, whilst the poultice shrinks onto the wall face. As the wall dries, water carrying the salts and contaminants in solution is drawn back to the surface by the high suction created by the fine pores in the poultice. The water evaporates and salts / contaminants precipitate within the poultice, which is left on the wall until it dries out; this may take several weeks, depending on the weather.

The poultice is then removed, taking the salt / contaminants with it.

Two or three cycles of poulticing may be required to reduce salt concentrations down to an acceptable level. This method has the advantage of rapid salt reduction with the poulticing.

## Packaging

Available in a 10l / 20kg tub.  The plastic used is suitable for recycling.  The sacrificial plaster is completely recyclable.

## Storage

This product can be stored in dry conditions and should be kept away from freezing conditions.  The shelf life is technically indefinite but realistically we would recommend use within 12 months.

## Health and Safety

| Risk Phrases | Safety phrases |
| --- | --- |
| R36/37/38 Irritating to eyes, respiratory system and skin | S2 Keep out of reach of children |
| R43 Contact with wet mortar may cause irritation, dermatitis and/or burns | S26 In case contact with eyes, rinse immediately with plenty water and seek medical advice. |
| R 66 Repeated exposure may cause skin dryness and cracking | S24/25 Avoid contact with skin and eyes |
|  | S36 Wear suitable protective clothing |

Declaration

This product contains no NHL or cement.

All Womersley’s products are manufactured under an ISO9001:2015 accredited factory production control system.